## Slide 1
Experimental results form the SDC measurements of the Samples:
180929-K3-2  3837
180930-K3-1  3839
180930-K3-2  3840
181001-K3-1  3841

## Slide 2
Measurement done with the SDC
20 Points were measured on each sample with an increment of 4.5 mm
On each point three electrochemical measurements were performed:
1. 1 LSV with a scan rate of 5 mV s-1 0.96 – 1.76 V vs. RHE
2. 20 CVs with a scan rate of 50 mV s-1 0.96 – 1.46 V vs. RHE (conditioning)
3. 3 LSV with a scan rate of 5 mV s-1 0.96 – 1.76 V vs. RHE
0.1 mol L-1 KOH pH 12.84
Reference electrode: Ag/AgCl 3 Mol L-1 KCl
Counter electrode : Pt wire
Measurement area : 0.007 cm-2

## Slide 3
Before Conditioning After Conditioning
Example Sample : 181001-K3-1 as deposited
0.1 mol L-1 KOH pH 12.84
Reference electrode: Ag/AgCl 3 Mol L-1 KCl
Counter electrode : Pt wire
Measurement area : 0.007 cm-2
Out of the LSVs from every measured sample the potentials at 1 mA cm-2 were taken for the next slides

## Slide 4
Comparison of the four different measured samples
Comparison of the potential measured at 1 mA cm-2
 Sample with the doping level of Fe offers the lowest potential
Fe
Co

## Slide 5
Sample : 180930-K3-1 as deposited
measured on 2018.11.23
Sample : 180929-K3-2 700°C 3h
measured on 2018.11.23
0.1 mol L-1 KOH pH 12.84
Reference electrode: Ag/AgCl 3 Mol L-1 KCl
Counter electrode : Pt wire
Measurement area : 0.007 cm-2

## Slide 6
Comparison of the two sample with a higher amount of Fe
potential measured at 1 mA cm-2
Points measured at the damaged spots from the depth measurement (These points can be excluded)
It seems that the heat treatment was not beneficial, since the obtained potentials are compared to the untreated sample higher.

## Slide 7
Sample : 181001-K3-1 as deposited
Measured on 2018.11.23
Sample : 180930-K3-2 as deposited
Measured on 2018.11.23
0.1 mol L-1 KOH pH 12.84
Reference electrode: Ag/AgCl 3 Mol L-1 KCl
Counter electrode : Pt wire
Measurement area : 0.007 cm-2

## Slide 8
Sample : 181001-K3-1 as deposited
Measured on 2018.11.23
Sample : 180930-K3-2 as deposited
Measured on 2018.11.23
0.1 mol L-1 KOH pH 12.84
Reference electrode: Ag/AgCl 3 Mol L-1 KCl
Counter electrode : Pt wire
Measurement area : 0.007 cm-2
Co3O4 - Observerd in the XRD measurement also visible in the CVs
Co 2+ /Co 3+ redox couple (∼1.1–1.3 V vs. RHE) – brought peak nearly not visible
Co 3+/Co 4+ redox couple at (∼1.4–1.55 V vs. RHE) – defined peak is visible in both CVs

## Slide 9
Comparison of the two sample with a low amount of Fe
potential measured at 1 mA cm-2
A clear trend of the potential in context with the amount of Fe can not be observed. Since the Sample 180930-K3-2 is offering a much higher potential for the same amount of Fe (2%) then the sample 181001-K3-1.