## Slide 1: Object Type Support Request on example of C04: Incorporating EDX Data in Research Data Management System
Victor Dudarev, Tobias Piotrowiak
Victor Dudarev
Project INF + C04:

## Slide 2: Agenda
EDX - Energy-Dispersive X-ray spectroscopy
    Data format description
    Search requirements
    EDX object type in RDMS:
      Validation
      Metadata extraction (composition range)
      Data extraction (all compositions)
    Search demonstration:
      EDX document
      Composition (measurement area)
    Plan proposal for data presentation
    Q&A.

## Slide 3: Material Characterisation: Chemical Entities Hierarchy
Chemical system
Crystal
modification
Heterogeneous mixture
Solution
…
Compound
System
(qualitative composition)
Modification
(crystal structure type)
Material
(quantitative composition)
…
Co-O
Co3O4
β-Co3O4
Crystal
modification
Crystal
modification
…
…

## Slide 4: Motivation: EDX as a “must have” characterisation
System
(qualitative composition)
Modification
(crystal structure type)
Material
(quantitative composition)
…
Co-O
Co3O4
β-Co3O4
known from synthesis
Energy-dispersive X-ray spectroscopy (EDX)
Analytical technique used
for the elemental analysis
or chemical characterization
of a sample
EDX
XRD
X-ray diffraction analysis (XRD)
technique used in to determine the crystallographic structure of a material (other story…)

## Slide 5: Combinatorial Materials Library: basic agreements
342 Measurement Areas (4.5 mm x 4.5 mm)
(x; y) coordinates on the surface
Materials Library Measurement Areas
I X Y
1 27000 4500
2 31500 4500
3 36000 4500
…
11 72000 4500
12 22500 9000
13 27000 9000
...
341 58500 90000
342 63000 90000

## Slide 6: EDX Measurement Outcome (Processed Data): the Table
Measurement Area Index Chemical Elements
[1, 342]
After processing one can conclude with the final outcome
https://dim.mdi.ruhr-uni-bochum.de/file/csv/6691
Composition for the Measurement Area 3 (atomic %)
V: 18.3 %
Mn: 4.8 %
Co: 17.2 %
Ni: 6.8 %
Ho: 53 %
Measurement Area 3
Composition Data

## Slide 7: Raw EDX data format (parseable text file)
Project: 0008081_EDXmapping ZGH (1)
Owner:
Site: Site of Interest 1
Sample: Sample 1
Type: Default
ID:
Processing option : All elements analysed
All results in atomic%
X and Y are stage positions
Spectrum In stats. X (mm) Y (mm) C O Si V Mn Co Ni Ho
Spektrum 1 {1} Yes -44.600 -40.300 80.36562 17.7799 0.331076 -0.3328189 9.434319E-02 1.12593 1.070188 -0.4342265
Spektrum 1 {2} Yes -40.100 -40.300 80.1367 23.03086 0.2024186 -4.792345E-02 -0.2482219 -3.621299 0.6450471 -9.758038E-02
Spektrum 1 {3} Yes -35.600 -40.300 83.67403 14.34433 0.2835474 -6.302138E-02 -7.115601E-02 1.043958 1.091217 -0.3029233
- … - … - … - … - … - … - … - … - … - … - … - …
Spektrum 1 {418} Yes 36.400 45.200 81.8801 12.53673 0.5853955 -1.528375E-02 4.889345E-02 -1.36448 6.783489 -0.4548477
Spektrum 1 {419} Yes 40.900 45.200 80.46669 12.32581 0.2078687 0.27237 -0.2769422 -7.077376 12.81309 1.268483
Spektrum 1 {420} Yes 45.400 45.200 83.68153 15.48148 0.0646082 0.2312067 -0.1969592 -2.165317 2.769571 0.1338789
Mean 43.79094 18.89702 29.09091 0.7714614 0.4576146 1.19483 3.057466 2.739753
Std. deviation 21.38218 7.121112 11.38863 0.9768385 0.3503809 20.70591 9.166298 3.695945
Max. 321.3774 82.92272 36.86385 3.61815 1.213754 225.3098 62.29993 5.617296
Min. -93.34522 -33.35334 -1.881486 -0.7680827 -0.4307786 -309.4584 -2.63329 -66.55944
Header (could be skipped)
Footer
(to skip)
Data we need (TAB separated). Almost, but:
420 measurement areas (instead of 342), need to filter;
Other elements (from substrate, need to filter: C, O, Si).

## Slide 8: Processed EDX data (good to go)
Index,V,Mn,Co,Ni,Ho
1,31.3,2.7,22.6,6,37.4
2,23.1,6.1,17,6.8,47
3,18.3,4.8,17.2,6.8,53
4,10,5.7,20.9,7.4,56
...
339,8.7,13,36.2,13.8,28.3
340,8.1,11,38.7,14.2,28
341,6.7,14.1,33.5,16.8,28.8
342,6.6,13,34.9,15.3,30.2
Even more open questions:
How to validate EDX data (raw&processed)?
What metadata for EDX should we store in RDMS?
How we would like to find our EDX data in RDMS?
Measurement Area Index Chemical Elements
[1, 342]
Good CSV document (processed)

## Slide 9: Validation Principle and Importance
Index,V,Mn,Co,Ni,Ho
1,31.3,2.7,22.6,6,37.4
2,23.1,6.1,17,6.8,47
3,18.3,4.8,17.2,6.8,53
4,10,5.7,20.9,7.4,56
...
339,8.7,13,36.2,13.8,28.3
340,8.1,11,38.7,14.2,28
341,6.7,14.1,33.5,16.8,28.8
342,6.6,13,34.9,15.3,30.2
Validator
Processed EDX CSV data
Project: 0008081_EDXmapping ZGH (1)
Owner:
Site: Site of Interest 1
Sample: Sample 1
Type: Default
ID:
Processing option : All elements analysed
All results in atomic%
X and Y are stage positions
Spectrum In stats. X (mm) Y (mm) C O Si V Mn Co Ni Ho
Spektrum 1 {1} Yes -44.600 -40.300 80.36562 17.7799 0.331076 -0.3328189 9.434319E-02 1.12593 1.070188 -0.4342265
Spektrum 1 {2} Yes -40.100 -40.300 80.1367 23.03086 0.2024186 -4.792345E-02 -0.2482219 -3.621299 0.6450471 -9.758038E-02
Spektrum 1 {3} Yes -35.600 -40.300 83.67403 14.34433 0.2835474 -6.302138E-02 -7.115601E-02 1.043958 1.091217 -0.3029233
- … - … - … - … - … - …
Spektrum 1 {418} Yes 36.400 45.200 81.8801 12.53673 0.5853955 -1.528375E-02 4.889345E-02 -1.36448 6.783489 -0.4548477
Spektrum 1 {419} Yes 40.900 45.200 80.46669 12.32581 0.2078687 0.27237 -0.2769422 -7.077376 12.81309 1.268483
Spektrum 1 {420} Yes 45.400 45.200 83.68153 15.48148 0.0646082 0.2312067 -0.1969592 -2.165317 2.769571 0.1338789
Mean 43.79094 18.89702 29.09091 0.7714614 0.4576146 1.19483 3.057466 2.739753
Std. deviation 21.38218 7.121112 11.38863 0.9768385 0.3503809 20.70591 9.166298 3.695945
Max. 321.3774 82.92272 36.86385 3.61815 1.213754 225.3098 62.29993 5.617296
Min. -93.34522 -33.35334 -1.881486 -0.7680827 -0.4307786 -309.4584 -2.63329 -66.55944
Raw EDX data
Some other data
1
2
3
Trust me,
I’m cute!
to Database
to Database

## Slide 10: Validation from RDMS perspective: API makes it flexible for all
API – Application Programming Interface
URL – Uniform Resource Locator
REST – REpresentational State Transfer
Provide a validator for every object type in configuration:
type: built-in type (object instantiated by class name);
https: URL to a REST Service (OpenAPI specification).
Validation result via external API call
{
"Code": 0,
"Message": null,
"Warning": null
}
{
"Code": 500,
"Message": "error text",
"Warning": null
}
type
invalid
valid
External service decision
type:TypeValidationLibrary.TypeValidator_EDX_CSV (interface IFileValidator)
https://validation.matinf.pro/edx/validation

## Slide 11: User perspective: how EDX should be findable?
After authorization (User group member):
https://dim.mdi.ruhr-uni-bochum.de/search/?typeid=13&pr0name=Mn&pr0type=Float&pr0min=15&pr0max=17&prcnt=1
https://dim.mdi.ruhr-uni-bochum.de/object/edx-csv-for-sample-8081-6691
Processed EDX CSV document should be findable by any chemical element concentration! We need to store (ConcentrationMIN; ConcentrationMAX) for every element present in the sample:
Sample 8081 (V-Mn-Co-Ni-Ho): fill properties
 | V | Mn | Co | Ni | Ho
Min | 0 | 0 | 0 | 0 | 20.7
Max | 36.4 | 16.1 | 46.5 | 19.1 | 100

## Slide 12: Metadata extraction: external API
Provide a data extractor for every object type in configuration:
type: built-in type (object instantiated by class name);
https: URL to a REST Service (OpenAPI specification).
type:TypeValidationLibrary.TypeValidator_EDX_CSV (interface IDatabaseValuesGetter)
https://validation.matinf.pro/edx/data
{ "DeletePreviousProperties": true,
"Properties": [
{ "PropertyId": 0,
"Type": 1,
"Name": "V",
"Value": 0,
"ValueEpsilon": null,
"SortCode": 10,
"Row": 1,
"Comment": "Minimal V content"
},
{ "PropertyId": 0,
"Type": 1,
"Name": "V",
"Value": 36.400001525878906,
"ValueEpsilon": null,
"SortCode": 10,
"Row": 2,
"Comment": "Maximal V content"
}
]
}
Administrative interface: Compositions
Metadata for EDX (range values):

## Slide 13: All data extraction: external API
Provide a data extractor for every object type in configuration:
type: built-in type (object instantiated by class name);
https: URL to a REST Service (OpenAPI specification).
type:TypeValidationLibrary.TypeValidator_EDX_CSV (interface IDatabaseValuesGetter)
https://validation.matinf.pro/edx/data
Data from EDX (all values == 342 compositions):
{
"CompositionElements": [
{ "CompoundIndex": 0, "ElementName": "V", "ValueAbsolute": null, "ValuePercent": 31.299999237060547 },
{ "CompoundIndex": 10, "ElementName": "Mn", "ValueAbsolute": null, "ValuePercent": 2.700000047683716 },
{ "CompoundIndex": 20, "ElementName": "Co", "ValueAbsolute": null, "ValuePercent": 22.600000381469727 },
{ "CompoundIndex": 30, "ElementName": "Ni", "ValueAbsolute": null, "ValuePercent": 6 },
{ "CompoundIndex": 40, "ElementName": "Ho", "ValueAbsolute": null, "ValuePercent": 37.400001525878906 }
],
"DeletePreviousProperties": true,
"Properties": [
{
"PropertyId": 0, "Type": 2, "Name": "Measurement Area", "Value": 1, "ValueEpsilon": null,
"SortCode": 0, "Row": null, "Comment": null
}
]
}

## Slide 14: Search for Composition (obtained from EDX)
Rubric: https://dim.mdi.ruhr-uni-bochum.de/rubric/p1project_ho-v-mn-co-ni-o_ho50_sample-id-0008081_measurement-areas
2) Search: https://dim.mdi.ruhr-uni-bochum.de/search/?system=Co-Ho-Mn-Ni-V&Copctmin=22&Copctmax=23&Hopctmin=37&Hopctmax=38&Mnpctmin=2&Mnpctmax=3&Nipctmin=6&Nipctmax=7&Vpctmin=31&Vpctmax=32

## Slide 15: Recommended plan for data presentation (for every project)
    Brief introduction to data / measurements
    Data format description
    Search requirements:
      How do you (partners) find your object among thousands of similar objects?
      What are essential parameters/properties?
    Proposal for object type in RDMS:
      File validation requirements (no validation -> formal schema)
      Metadata extraction or template proposal (enlist mandatory properties)
      Data extraction (if required, specify requirements)
    Q&A.

## Slide 16: A Perfect “Object Type Support Request” from … project
    based on considered EDX example…
    comes from the next slide

## Slide 17: Brief introduction to data / measurements: coordinate grid
342 Measurement Areas (4.5 mm x 4.5 mm)
(x; y) coordinates on the surface
Materials Library Measurement Areas
I X Y
1 27000 4500
2 31500 4500
3 36000 4500
…
11 72000 4500
12 22500 9000
13 27000 9000
...
341 58500 90000
342 63000 90000

## Slide 18: Data format description: raw EDX data format
Project: 0008081_EDXmapping ZGH (1)
Owner:
Site: Site of Interest 1
Sample: Sample 1
Type: Default
ID:
Processing option : All elements analysed
All results in atomic%
X and Y are stage positions
Spectrum In stats. X (mm) Y (mm) C O Si V Mn Co Ni Ho
Spektrum 1 {1} Yes -44.600 -40.300 80.36562 17.7799 0.331076 -0.3328189 9.434319E-02 1.12593 1.070188 -0.4342265
Spektrum 1 {2} Yes -40.100 -40.300 80.1367 23.03086 0.2024186 -4.792345E-02 -0.2482219 -3.621299 0.6450471 -9.758038E-02
Spektrum 1 {3} Yes -35.600 -40.300 83.67403 14.34433 0.2835474 -6.302138E-02 -7.115601E-02 1.043958 1.091217 -0.3029233
- … - … - … - … - … - … - … - … - … - … - … - …
Spektrum 1 {418} Yes 36.400 45.200 81.8801 12.53673 0.5853955 -1.528375E-02 4.889345E-02 -1.36448 6.783489 -0.4548477
Spektrum 1 {419} Yes 40.900 45.200 80.46669 12.32581 0.2078687 0.27237 -0.2769422 -7.077376 12.81309 1.268483
Spektrum 1 {420} Yes 45.400 45.200 83.68153 15.48148 0.0646082 0.2312067 -0.1969592 -2.165317 2.769571 0.1338789
Mean 43.79094 18.89702 29.09091 0.7714614 0.4576146 1.19483 3.057466 2.739753
Std. deviation 21.38218 7.121112 11.38863 0.9768385 0.3503809 20.70591 9.166298 3.695945
Max. 321.3774 82.92272 36.86385 3.61815 1.213754 225.3098 62.29993 5.617296
Min. -93.34522 -33.35334 -1.881486 -0.7680827 -0.4307786 -309.4584 -2.63329 -66.55944
Header (could be skipped)
Footer
(to skip)
Data we need (TAB separated). Almost, but:
420 measurement areas (instead of 342), need to filter;
Other elements (from substrate, need to filter: C, O, Si).

## Slide 19: EDX: what we need to extract (the Table)
Measurement Area Index Chemical Elements
[1, 342]
After processing one can conclude with the final outcome
https://dim.mdi.ruhr-uni-bochum.de/file/csv/6691
Composition for the Measurement Area 3 (atomic %)
V: 18.3 %
Mn: 4.8 %
Co: 17.2 %
Ni: 6.8 %
Ho: 53 %
Measurement Area 3
Composition Data

## Slide 20: Search requirements: how EDX should be findable?
After authorization (User group member):
https://dim.mdi.ruhr-uni-bochum.de/search/?typeid=13&pr0name=Mn&pr0type=Float&pr0min=15&pr0max=17&pr1name=V&pr1type=Float&pr1min=36&pr1max=40&prcnt=2
We need to store (ConcentrationMIN; ConcentrationMAX) for every element:
1) EDX document should be findable by chemical elements contents within a range in materials library

## Slide 21: Search requirements: individual compositions findability
After authorization (User group member):
https://dim.mdi.ruhr-uni-bochum.de/search/?system=Co-Mn-V&Copctmin=30&Copctmax=32&Mnpctmin=3&Mnpctmax=5&Vpctmin=27&Vpctmax=29
We need to create composition for every measurement area of materials library on basis of EDX data. For example:
Composition (MA 119) from EDX CSV for sample 8081
2) Compositions within measurements area should be findable

## Slide 22: Validation Requirements
Index,V,Mn,Co,Ni,Ho
1,31.3,2.7,22.6,6,37.4
2,23.1,6.1,17,6.8,47
3,18.3,4.8,17.2,6.8,53
4,10,5.7,20.9,7.4,56
...
339,8.7,13,36.2,13.8,28.3
340,8.1,11,38.7,14.2,28
341,6.7,14.1,33.5,16.8,28.8
342,6.6,13,34.9,15.3,30.2
Processed EDX CSV data
Project: 0008081_EDXmapping ZGH (1)
Owner:
Site: Site of Interest 1
Sample: Sample 1
Type: Default
ID:
Processing option : All elements analysed
All results in atomic%
X and Y are stage positions
Spectrum In stats. X (mm) Y (mm) C O Si V Mn Co Ni Ho
Spektrum 1 {1} Yes -44.600 -40.300 80.36562 17.7799 0.331076 -0.3328189 9.434319E-02 1.12593 1.070188 -0.4342265
Spektrum 1 {2} Yes -40.100 -40.300 80.1367 23.03086 0.2024186 -4.792345E-02 -0.2482219 -3.621299 0.6450471 -9.758038E-02
Spektrum 1 {3} Yes -35.600 -40.300 83.67403 14.34433 0.2835474 -6.302138E-02 -7.115601E-02 1.043958 1.091217 -0.3029233
- … - … - … - … - … - …
Spektrum 1 {418} Yes 36.400 45.200 81.8801 12.53673 0.5853955 -1.528375E-02 4.889345E-02 -1.36448 6.783489 -0.4548477
Spektrum 1 {419} Yes 40.900 45.200 80.46669 12.32581 0.2078687 0.27237 -0.2769422 -7.077376 12.81309 1.268483
Spektrum 1 {420} Yes 45.400 45.200 83.68153 15.48148 0.0646082 0.2312067 -0.1969592 -2.165317 2.769571 0.1338789
Mean 43.79094 18.89702 29.09091 0.7714614 0.4576146 1.19483 3.057466 2.739753
Std. deviation 21.38218 7.121112 11.38863 0.9768385 0.3503809 20.70591 9.166298 3.695945
Max. 321.3774 82.92272 36.86385 3.61815 1.213754 225.3098 62.29993 5.617296
Min. -93.34522 -33.35334 -1.881486 -0.7680827 -0.4307786 -309.4584 -2.63329 -66.55944
Raw EDX data
1
2

## Slide 23: Metadata extraction
Task: Metadata extraction or template proposal (enlist mandatory properties) - No template or fixed properties list - Property names are chemical elements that are in a sample - For every element should be created two Float properties with minimal and maximal contents
(ConcentrationMIN; ConcentrationMAX) for every element
 | V | Mn | Co | Ni | Ho
Min | 0 | 0 | 0 | 0 | 20.7
Max | 36.4 | 16.1 | 46.5 | 19.1 | 100

## Slide 24: Data extraction
It’s required to create objects of Composition type for every measurement area (342)
For example
and these compositions should be connected with “parent” objects:
Source EDX CSV object
Source sample
https://dim.mdi.ruhr-uni-bochum.de/object/measurement-area-001-from-edx-csv-for-sample-8081-12866

## Slide 25: Thanks for your kind attention
Q&A
Victor Dudarev
Victor.Dudarev@rub.de
https://vdudarev.ru